## Slide 1
Master Thesis
Analysis of the Failure Behavior of Carbon Fibre Reinforced Polymer Open Hole Tensile Test Specimens
Submitted/Presented by: | Apurv Kulkarni
Matriculation Number: | 4815274
Degree Program: | Computational Modelling and Simulation
Field of Study: | Computational Engineering
Date of Submission: | 4 May 2021
Place and Date: | Dresden, 26 May 2021
Faculty of Mechanical Engineering - Institute of Solid Mechanics
Chair of computational and Experimental Solid Mechanics

## Slide 2
Contents
Motivation
Basics
  Material model
  Design of experiments and Sensitivity analysis
Numerical Experiments
  Framework
  Results
Conclusion

## Slide 3
1. Motivation
Notes: 3

## Slide 4: 1. Motivation
Carbon Fibre Reinforced Polymer Composites (CFRP)
  Heterogeneous systems
    Reinforcement ► Carbon Fibre
      High specific strength
    Matrix ► Epoxy resin
      Binding fibres and load transmission
Properties
  High strength
  High stiffness
  Low weight
Applications
Reinforcement material
Carbon Fibre
Carbon Fibre “Plain Weave”
CFRP board
[1]
[2]
[3]
[4]
[5]
[6]
Mechanical Joints

## Slide 5: 1. Motivation
Open hole tensile (OHT) testing
Failure in CFRP
  Material composition – volume fraction, component properties
  Geometry
  Orientation/Layup
  Loading conditions
[7]
x
y
1
2
Orthotropic materials*

## Slide 6: 1. Motivation
Objective:
Perform analysis to understand the influence of material parameters
and notch geometry on an open hole specimen under tensile loading.

## Slide 7: 1. Motivation
Objective:
Perform analysis to understand the influence of material parameters
and notch geometry on an open hole specimen under tensile loading.
Scope:
  Understanding failure in CFRP structures,
[8]
[9]
Matrix crack
Fibre fracture
Delamination
Matrix crack
90o
0o

## Slide 8: 1. Motivation
Objective:
Perform analysis to understand the influence of material parameters
and notch geometry on an open hole specimen under tensile loading.
Scope:
  Understanding failure in CFRP structures,
  Designing computer experiments,
[8]
[9]
Experiment | Design Variables |  |  |  | 
 | X1 | X2 | … | … | Xn
e1 | x11 | x12 | … | … | x1n
e2 | x21 | x22 | … | … | x2n
… | … | … | … | … | …
ep | x1p | x2p | … | … | xnp

## Slide 9: 1. Motivation
Objective:
Perform analysis to understand the influence of material parameters
and notch geometry on an open hole specimen under tensile loading.
Scope:
  Understanding failure in CFRP structures,
  Designing computer experiments,
  Creating workflow,
Designing
experiments
Running
experiments
Data extraction
Data
analysis

## Slide 10: 1. Motivation
Objective:
Perform analysis to understand the influence of material parameters
and notch geometry on an open hole specimen under tensile loading.
Scope:
  Understanding failure in CFRP structures,
  Designing computer experiments,
  Creating workflow,
  Statistical analysis.

## Slide 11
2. Basics
Notes: 11

## Slide 12: 2.3 Material Model
Composite material model proposed by Pinho et al.[16]
  Fibre tensile failure:
  Fibre compression failure (Kinking):
  Matrix tensile failure:
  Matrix compressive/shear failure:
  Continuum damage model
Fracture angle
Fracture angle
Notes: Possible question: what is physically based criteria and how It is different from non-physically based criteria

## Slide 13: 2.3 Material Model
Inter-laminar material modelling proposed by Benzeggagh-Kenane[17]
  Zero thickness cohesion elements
  Failure criteria – relative displacements, δ
    Mode I (Tension):
    Mode II (Shear):
    Mode III (2nd Shear):
Mode I
Mode II
Mode III
Traction Separation Law Curve (TSLC)
Cohesion element

## Slide 14: 2.4 Design of Experiments and Sensitivity Analysis
Design of experiments
  Latin hypercube design (LHD)
    No. of experiments independent of no. of design variables
    Fewer experiments required
    Optimal design
Sensitivity analysis
  Linear Regression analysis
    Bivariate
    Multiple
  Pearson’s correlation coefficient (PCC)
    PCC = +/- 1 → Strong correlation
    PCC = 0 → No correlation
  Spearman’s ranked correlation coefficient (SRCC)
    SRCC = +/-1 → monotonous relation
    SRCC = 0 → no relation
System/Model/Process
Design
variables
Response
variables
Optimal

## Slide 15
3. Experiment Framework
Notes: 15

## Slide 16: 3.1 Workflow
Designing
experiment
Running
experiments
Data extraction
Data analysis

## Slide 17: 3.1 Workflow
Designing
experiment
Running
experiments
Data extraction
Data analysis
Define
objective
Identifying input variables
Building design matrix using LHD
Creating LS-Dyna
material and geometry cards
[18]

## Slide 18: 3.1 Workflow
Designing
experiment
Running
experiments
Data extraction
Data analysis
Create sbatch files for submitting jobs on HPC
Run computer experiments using
LS-Dyna analysis software
[18]

## Slide 19: 3.1 Workflow
Designing
experiment
Running
experiments
Data extraction
Data analysis
Identifying output variables
Data extraction from results using LS-Prepost macros
Data cleaning
[18]
[19]
[20]

## Slide 20: 3.1 Workflow
Designing
experiment
Running
experiments
Data extraction
Data analysis
Bivariate Regression analysis
Correlation analysis
Multiple regression analysis
Drawing conclusion
[19]
[20]
[22]
[23]
[21]

## Slide 21: 3.2 FEM Model
Six layers symmetrically arranged
  Configuration – [0/90/0/90/0/90]s
  Zero thickness element between each layer
Mesh selection
  3 elements in thickness in each layer
  Convergence analysis ►140 elements
Boundary conditions on nodes
240
50
120
50
Clamping
area
Clamping area
19 mm in thickness
All dimensions are in mm
28.8
Ry = 48
Rx
Symmetric
Zero thickness cohesive layers
Fixed nodes
Prescribed motion

## Slide 22: 3.3 Experiment Parameters
Design variables (Input parameters)
Strength | XT | Longitudinal tensile strength
 | XC | Longitudinal compressive strength
 | YT | Transverse tensile strength
 | YC | Transverse compressive strength
 | SL | Longitudinal shear strength
MANG
Ry
Rx
NOTCHR =
Rx
Ry
where, Ry = 48mm
Other | EFS | Maximum effective strain for element layer failure
 | SIGY | In-plane shear yield stress
 | FIO | Fracture angle in pure transverse compression
 | T | Peak traction in normal direction mode
 | S | Peak traction in tangential direction mode
Fracture toughness | ENKINK | Fracture toughness for longitudinal (fibre) compressive failure mode
 | ENA | Fracture toughness for longitudinal (fibre) tensile failure mode
 | ENB | Fracture toughness for intralaminar matrix tensile failure
 | ENT | Fracture toughness for intralaminar matrix transverse shear failure
 | ENL | Fracture toughness for intralaminar longitudinal shear failure
 | GI | Fracture toughness mode I
 | GII | Fracture toughness mode II
Geometry | MANG | Misalignment angle of material orientation
 | NOTCHR | Notch radius ratio Rx/Ry with Ry=48mm
Moduli, poisons ratio and Density | EA | Young’s modulus in longitudinal direction
 | EB | Young’s modulus in transverse direction
 | EC | Young’s modulus in through thickness direction
Moduli, poisons ratio and Density | GAB | Shear modulus plane ab
 | GCA | Shear modulus plane ca
 | GBC | Shear modulus plane bc
 | PBA | Poisson’s ratio in ba
 | PCA | Poisson’s ratio in ca
 | PCB | Poisson’s ratio in cb
 | RHO | Mass density of composite material
 | RHOC | Mass density of cohesive layer

## Slide 23: 3.3 Experiment Parameters
Correlation between design variables – minimum correlation

## Slide 24: 3.3 Experiment Parameters
Response variables (Output parameters)
gMAS | Maximum applied stress in x-direction before failure
gMLS | Maximum longitudinal stress globally at maximum gMAS
gMTS | Maximum transverse stress globally at maximum gMAS
gMPS | Maximum principle stress globally at maximum gMAS
gMSS | Maximum shear stress globally at maximum gMAS
gMIPSS | Maximum in-plane shear stress globally at maximum gMAS
SC | Stress concentration factor at the notch at maximum gMAS
Applied stress (MPa)
Time (sec)
Maximum applied
stress (gMAS)
1e8

## Slide 25
4. Results
Notes: 25

## Slide 26: 4.1 Bivariate Analysis
Pearson’s
correlation coefficient
Spearman’s ranked correlation coefficient

## Slide 27: 4.1 Bivariate Analysis
Influence of Longitudinal Tensile Strength (XT)
Influence of Misalignment Angle (MANG)
x
y
a
b
MANG
gMAS | Maximum applied stress in x-direction before failure
gMLS | Maximum longitudinal stress globally at maximum gMAS
gMIPSS | Maximum in-plane shear stress globally at maximum gMAS

## Slide 28: 4.1 Bivariate Analysis
Influence of Notch Radius Ratio (NOTCHR)
gMAS | Maximum applied stress in x-direction before failure
SC | Stress concentration factor at the notch at maximum gMAS
Rx
Ry=48mm
NOTCHR =
Rx
Ry

## Slide 29: 4.2 Multiple Linear Regression Analysis
Coefficient values ( )
Higher coefficient values for XT, YT, GI, GII, MANG and NOTCHR
Regression summary - gMAS
Higher t-value and lower P-value suggests good validity of the parameter
Notes: What is t-value and p-value?

## Slide 30
5. Conclusion

## Slide 31: 5.1 Conclusion
Analysis is results have shown moderate to strong dependency with:
  Loading type → Tensile parameters are more dominating (XT, YT)
  → Inter laminar shear dominating (GII)
  Material orientation w.r.t loading direction → MANG
  Geometry of specimen → NOTCHR
Non-significant correlation values for parameters like moduli, Poisson’s ratio, fracture toughness, etc.
  Not selecting appropriate response variables
  Smeared effect due to complex behavior of failure in composites
Future work :
  Studying experiments with different response variables
  Meta modelling using neural networks (reducing time for entire simulation)
Notes: 31

## Slide 32: 5.1 Conclusion
Physics simulation + Exploratory data analysis
Manufacturing defects
  MANG, NOTCHR
  Deviation in material properties
Important parameters
  Less influencing
  More influencing
Limitations
  Material model
  Analysis software suit
Future work
  Studying experiments with different response variables
  Meta modelling using neural networks (reducing time for entire simulation)
Notes: 32

## Slide 33: References
[1] Can Carbon Fiber Replace Steel in the Automotive Industry? by KaganPittman. url: https://www.engineering.com/story/can-carbon-fiber-replace-steel-inthe-automotive-industry,
[2] https://www.compositesworld.com/articles/more-from-jec-high-quality-carbon-fiber-monocoques-in-two-hours [3]
[3] https://www.nextbigfuture.com/2016/06/fourth-generation-composites-used-for.html
[4] https://www.engadget.com/superstrata-ion-terra-3d-printed-carbon-fiber-electric-bike-140050711.html?
[5] https://www.jmfiber.com/portfolio/carbon-fiber-tennis-racket
[6] https://www.sciencedirect.com/science/article/pii/S0263822307001341
[7] O’Higgins, R. M., McCarthy, M. A. and McCarthy, C. T. Comparison of open hole tension characteristics of high strength glass and carbon fibre-reinforced composite materials. Composites Science and Technology. Directions in Damage and Durability of Composite Materials, with regular papers 68.13, Oct. 2008, pp. 2770–2778.
[8] Davies, G A O and Olsson, R. Impact on composite structures. THE AERONAUTICAL JOURNAL, 2004, p. 23
[9] Figure 7.4 Micrographic matrix cracking in multidirectional laminate [20]. url: https: //www.researchgate.net/figure/Micrographic-matrix-cracking-in-multidirectionallaminate-20_fig4_325024206
[10] Daniel, Isaac M. and Ishai, Ori. Engineering mechanics of composite materials. 2nd ed. New York: Oxford University Press, 2006. isbn: 978-0-19-515097-1.
[11] Figure 7.4 Micrographic matrix cracking in multidirectional laminate [20]. url: https: //www.researchgate.net/figure/Micrographic-matrix-cracking-in-multidirectionallaminate-20_fig4_325024206.
[12] Suresh, Masa et al. Fractographic Analysis of Tensile Failures of Aerospace Grade Composites. Materials Research 15, Dec. 2012, pp. 990–997.

## Slide 34: References
[13] Brauer, Delia et al. Degradable phosphate glass fiber reinforced polymer matrices: Mechanical properties and cell response. Journal of materials science. Materials in medicine 19, Feb. 2008, pp. 121–7.
[14] Han, Geng et al. The failure mechanism of carbon fiber-reinforced composites under longitudinal compression considering the interface. Science and Engineering of Composite Materials 24.3, May 2017, pp. 429–437.
[15] Zanjani, Jamal Seyyed Monfared et al. Nano-engineered design and manufacturing of high-performance epoxy matrix composites with carbon fiber/selectively integrated graphene as multi-scale reinforcements. RSC Advances 6.12, Jan. 2016, pp. 9495–9506.
[16] Pinho, S.T., Iannucci, L. and Robinson, P. Physically-based failure models and criteria for laminated fibre-reinforced composites with emphasis on fibre kinking: Part I: Development. Composites Part A: Applied Science and Manufacturing 37.1, Jan. 2006, pp. 63–73.
[17] Benzeggagh, M.L. and Kenane, M. Measurement of mixed-mode delamination fracture toughness of unidirectional glass/epoxy composites with mixed-mode bending apparatus. Composites Science and Technology 56.4, 1996, pp. 439–449.
[18] LS-DYNA | Livermore Software Technology Corp. url: http://www.lstc.com/products/ls-dyna
[19] https://numpy.org/
[20] https://pandas.pydata.org/
[21] https://seaborn.pydata.org/#
[22] https://www.scipy.org/
[23] https://www.statsmodels.org/stable/index.html

## Slide 35
Thank you for your attention !!

## Slide 36
Backup slides
Notes: 36

## Slide 37: 2.1 Damages in an OHT specimen
Cross-ply laminate under tensile loading:
Damage initiation from notch
[0/90/0]
Stresses along x-axis

## Slide 38: 2.1 Damages in a OHT specimen
Delamination
[15]
Matrix Cracking
[11]
Fibre-Matrix Debonding
[12]
Fibre Fracture
Kinking
[14]
[13]

## Slide 39: Convergence analysis
Convergence analysis on 00 UD ply
  140 elements on the notch circumference
0 1 2 3 4
Design Points
Time (sec)
Applied stress (MPa)
1.52%
12.73%
11.70%
19.23%
0
1
2
3
4
21.10%
19.94%
4.35%
0.19%
Stress concentration factor
Design Points

## Slide 40: Material model by Pinho et al.
Fibre tensile failure:
Fibre compression failure (Kinking):
Matrix tensile failure:
Matrix compressive/shear failure:
Notes: Possible question: what is physically based criteria and how It is different from non-physically based criteria

## Slide 41: Material model by Pinho et al.
Fibre compression failure (Kinking):
Notes: Possible question: what is physically based criteria and how It is different from non-physically based criteria

## Slide 42: Material model by Pinho et al.
Continuum damage model
Notes: Possible question: what is physically based criteria and how It is different from non-physically based criteria

## Slide 43: Linear Regression and Sensitivity analysis
Regression
  Fitting line –
  Error –
  Objective –
  R-Squared –
  PCC –
R-Squared = PCC2

## Slide 44: Full heatmap Bivariate analysis
Pearson’s correlation coefficient (PCC) heatmap

## Slide 45: Bivariate analysis – Full heatmap
Spearman’s ranked correlation coefficient (SRCC) heatmap

## Slide 46: Heatmap when all parameters are varied equally

## Slide 47: 2.1 Analysis of composite
Multi-Scale analysis
Composite material as an orthotropic material.
Tensile loading direction and Fibre direction in a lamina
  Loading parallel to fibre direction
    Fibres take major loads
  Loading non-parallel to fibre direction
    As increases, load shifts towards matrix
Mesoscopic Level
x
y
1
2
[10]
Notes: Orthotropic material
→Subset of anisotropic material (at meso scale).
→3 material axes of symmetry
→Material Properties are direction dependent